| Product Description | TOTTF is a new Generation Water Based Exterior/Interior Long Life Structured Scratch Plaster Type Textured Render/Coating that contains distinct scratch marks or grooves. Its main use is for the long Term Protection of buildings |
| --- | --- |
| Application Areas | Interior and exterior. Cement tiles (new or weathered), fibre cement sheeting (new or weathered), Plaster, previously painted substrates. Primed metal and wooden substrates. |
| Product Features | Highly durable and UV resistant for the Harsh South African climate Scratch plaster effect to hide surface imperfections Water resistance Excellent adhesion Excellent application properties Quick drying Low odour If correctly applied to a properly prepared substrate the product has a life expectancy of 7-10 years, possibly longer The product has been “independently” tested using a range of relevant Local (SANS) and international (CGRI/ASTMS and ISO) Test methods to ensure that its performance meets the exacting demands of their customers. The Tests methods/Standards used include: ASTMS 4060/D4828/E96/G53 CGRI Wet abrasion ISO1519/2409/12040 SANS 146/170/1586 (SANS 1586 Only Product Relevant Requirements) Comes in various stone sizes to give different effects and film builds |
| Product Data | Resin Base | Acrylic resin emulsion |
|  | Drying Time | Touch dry: ± 4-6 hour Recoating time 16-24 Hours |
|  | Film Thickness | 1-2.5 MM per coat |
|  | Spreading Rate | 8-12 SQM/ 20 Litre depending on the stone size and the Porosity of the Substrate |
| Application Details |  |
| Mixing | Always stir well before use with a flat paddle. |
| Application Method | Trowel only |
| Thinning | This Product is ready for use un-thinned; thinning with water will reduce its hiding power./reduce the effect |
| Cleaning | Application equipment clean up is with clean tap water. |
| Application | Stir well before use. With a trowel, apply a generous/thick but even coat of TOTTF to the area that needs protecting in small manageable sections. Allow to dry overnight Normally a second coat is not required but sometimes in very dusty areas a dirt Repellant Clear coat (TOTCC) is required This Product is ready for use un-thinned; thinning with water will reduce its hiding power and effectiveness. Application equipment clean-up is with clean tap water. Do not apply before 09:00 and after 16:00 in the winter. Do not apply exterior if it looks like rain will occur within 4-6 hours of application.. |
| Surface Preparation |  |
| Rusted Metal | Affected areas need to be cleaned back to bright metal and spot primed with Water based Metal Primer. Remove collected sand and dust from the area. Apply a Coat of TOTTF |
| New Metal | Degrease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free. Rinse well with potable water. Prime the Clean Degreased Metal with a water based Metal Primer Apply a coat of TOTTF |
| Uncoated cement Plaster surfaces | Remove dust, foreign material, fungal and algae growth. Fill all visible cracks and seal with WB Plaster Primer. Apply a coat of TOTTF |
| Fibre Cement Surfaces (Uncoated, Weathered or New) | Remove dust, foreign material, fungal and algae growth. If friable or powdery, seal with Bonding or WB Plaster Primer Apply a coat of TOTTF |
| Previously Painted Surfaces | Make sure old paint coatings are firm and sound Remove all loose, flaking and bubbling paint. Remove all dust, grease, foreign material, fungal and algae growth. Allow to dry. If then powdery or friable, seal with Bonding Liquid or WB Plaster Primer Apply a coat of TOTTF |
| Colour Range and Quantities | This Product is available in white and a large range of Colours and Texture levels (1,1 to 2.4MM) Available in 20litres. Only |
| Precautions | This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations). |
| Disclaimer | Trowel on Textures cannot be held liable if the product fails due to improper surface preparation or application. |
| Trowel on Textures |
| 016-9310118 | www.trowel-on-textures.co.za |